## Slide 1
Kinetic Monte Carlo study of TDDB in STTMRAM MgO

## Slide 2: Agenda
Device
Literature
Hypothesized models and assumptions
Objectives of Atomistic simulation
Contribution and Novelty
Kinetic Monte Carlo Simulation and Equations
KMC discussion on 31 Jan 22
Potentially add TEM data from GF

## Slide 3: Device
Study the breakdown of this
Voltages used 0.7-0.9V

## Slide 4: Literature
UNI vs BIP pulsing MTTF
Self-heating
Strain effects
V+
0V
V-
BIP
2018 Sankaran et al. Evidence of Magnetostrictive Effects on STT-MRAM Performance by Atomistic and Spin Modeling
2014 Naik et al. Effect of electric-field on the perpendicular magnetic anisotropy and strain properties in CoFeB/MgO magnetic tunnel junctions
Main difference in UNI+ and UNI- MTTF could be accounted for with SH.
BIP still very different.
Mean-time-to-failure BIP<<UNI
Simulation of Self-heating in the MgO
Piezoelectric effect causing strain fatigue
Strain causes uneven resistance and other effects (simulation)
Why BIP is not avg(UNI- and UNI+)?

## Slide 5: Literature
4. Defect DFT studies
El-Sayed et al. 2018 Effect of electric field on migration of defects in oxides: Vacancies and interstitials in bulk MgO
McKenna et al. 2009 First-principles calculations of defects near a grain boundary in MgO
Bean et al. 2018 Stability of point defects near MgO grain boundaries in FeCoB/MgO/FeCoB magnetic tunnel junctions
Fang-Guang Kuang et al. 2017 An ab initio study on the electronic and magnetic properties of MgO with intrinsic defects
(a) Change in electron density of the F0 center along its migration pathway. The red and light pink spheres are O and Mg, respectively (b)Values of the migration barriers of F centers in MgO as an electric field is applied.
Ramesh et al. 2021 Insertion Trade-off Effects on the Spin-Transfer Torque Memory Explored by In Situ X-ray
Mg insertion layer between MgO-CoFeb interface changing crystallinity and defect formation. Improved TDDB but worsened magnetism.
Fei Guo et al. 2018 Strong anti-strain capacity of CoFeB/MgO interface on electronic
structure and state coupling
0% strain
3.5% strain
Majority Δ1 Spin Bloch State

## Slide 6: Literature Review
Mahmoud et al., CNRS, 2021, Diffusion mechanism of bound Schottky defect in magnesium oxide
El-Sayed et al. 2018 Effect of electric field on migration of defects in oxides: Vacancies and interstitials in bulk MgO
Carboni et al. 2018 Modeling of Breakdown-Limited Endurance in Spin-Transfer Torque Magnetic Memory Under Pulsed Cycling Regime

## Slide 7: Model 1: Combined two-step breakdown model
CoFeB
MgO
UNI+
e-
e-
e-
e-
CoFeB
U1
U2
U3
CoFeB
MgO
BIP
e-
e-
e-
e-
CoFeB
e-
e-
e-
e-
B1a
B2
B1b
UNI mode
U1. Interface defects (ID) form.
U2. IDs reduce activation energy for bulk defect (BD) U3. BD triggers the final defect at other interface.
BIP mode
B1ab. IDs form, accelerated by strain fatigue.
B2. IDs at both side drastically reduce activation energy for BD. Hence, MTTF for BIP << UNI+/-.
*Supplementary info in appendix

## Slide 8: Model 2: UNI TDDB mechanism (Release-Reaction model)
CoFeB
(+) anode
MgO
CoFeB (-) cathode
: O vacancy or Boron
2. Diffusion of Defect
1. Release of Defect
3. Reaction of Defect
To do:
Current density plots with SH correction
Still unsure:
Single or multi domain crystal
3-4 monolayers
*Supplementary info in appendix

## Slide 9: Model 2: BIP TDDB mechanism
CoFeB
MgO
CoFeB
: O vacancy or B
2. UNI-, defect displaces up
1. UNI+, defect displaces up
Resultant zero net displacement
Possible experiments to rule out model:
Asymmetric BIP will lead to net diffusion.
Varying PW, might get to PW>diffusion time constant. If PW long enough, defect can diffuse over in one PW. Caution: if PW too long, might hit VBD.
Check if compressive + tensile strains can account for order of magnitude decrease in MTFF. Can we think of it as a spring? Check flexible electronics.
Supporting info:
According to Macpherson's paper, the effects of external field scale to the equation (2+k)/3 (valid for cubic and amorphous dielectrics), where k is dipole moment. That means MgO has 9/5 to 12/5 times more field effect than SiO2. The effective field in the MgO is 16-20MV/cm.
Check if MgO is Ferroelectric?
Look at how piezoelectrics fail for mechanical failure.
Check Crystallization/Annealing temperature of MgO. Can we use TMR to gauge crystallinity in MgO.
Check dzz meaning with Naik.
Explore Asymmetric BIP DOE before send out!!!
O
M
O
M
O
M
O
M
O
M
O
M
*Supplementary info in appendix

## Slide 10: Model 2: Why BIP is still power law
CoFeB
MgO
CoFeB
: O vacancy or B
1. At initial time, there are a few defects in MgO.
CoFeB
MgO
CoFeB
: O vacancy or B
2. Defects are generated overtime, but most have zero net-displacement. This lowers the resistance of the oxide due to trap-assisted tunneling.
CoFeB
MgO
CoFeB
Random walk
3. At a threshold concentration of defects, some defects make it to the interface via random walk or in one PW. This weakens the oxide and lowers resistance.
: O vacancy or B
One PW
CoFeB
MgO
CoFeB
4. The falling resistance leads to higher current, and more defects make it across. A positive feedback loop that leads to more abrupt failure.
: O vacancy or B

## Slide 11: Possible objectives for Atomistic simulation
Does the presence of an oxygen vacancy in MgO make it easier for another defect to be created in the vicinity? If so, by how much could the activation energy reduce?
How does interfacial strain (tensile / compressive) affect the activation energy needed for Mg-O bond breaking?
How much lower could the activation energy for Mg-O bond breaking be at a grain boundary site as compared to a bulk grain site?
How does MgO bond energy-level excite with temperature? (refer to Fig 5. Wu et al. 2013 Generalized hydrogen release-reaction model for the breakdown of modern gate dielectrics)
Are the defects Boron-based interstitials or Oxygen vacancies? We suspect that O vac. are more likely. Stack is likely to be under-oxidized, so likely to have some O-vac at initial state.
Are defects more likely to spread via Model 1 Adjacent defect induced formation or Model 2 diffusion/drift?

## Slide 12: What we know
Experimental ΔTSH increase fits well with Zunaid’s simulation
C is obtained by manual tweaking to fit Zunaid’s curve. This is still non-trivial as R decreases with V (especially RAP) so not expected to fit perfectly.
C is uniform for a given CD and Tambient.
PW is tricky to simulate. C should be uniform for given PW. Naga has suggested simulating ΔTSH vs. PW, still thinking about it. Zunaid has simulated with a different/normalized PW that produces comparable ΔTSH. I’m not sure of details.
Chart: Voltage (V)
UNI+ AP state
UNI- P state
 | P | AP
65 | 0.43 | 0.69
77 | 0.41 | 0.54
88 | 0.38 | 0.54
Table 1. C vs CD and Polarity
Dots are expt
Line is sim
Dots are expt
Line is sim

## Slide 13: What we know
Main difference in UNI+ and UNI- MTTF could be accounted for with SH.
BIP still very different.
Unsure BIP SH correction due to switching.
+109C is from averaging ΔTSH of UNI- and UNI+.
+125C is from worst case (ie. P state).
MTTF trend seems non-Arrhenius… more on that later
Before UNI- SH correction
After SH correction
Note: PW=200ns throughout this presentation!
*key plots

## Slide 14: What we know
Power Law Exponent decreases with temperature
Power Law Exponent no specific trend with device area
(How power law comes about) FIG. 5. Schematics of the thermally assisted hydrogen release model. When Si-H bond is in the ground state at T¼0 C (a), Si-H breakage occurs through excitation over all the energy-levels by electrons. When Si-H bond is excited to higher energy states at finite temperatures (b), the number of energy levels for bond breakage are reduced, leading to smaller exponents since the power-law exponents is equal to 4N.9–12 This new model explains the reduction of the power law exponent with increasing temperature.

## Slide 15: Open question 1: Arrhenius or not?
*Lines are visual aids
NO: trend is non-linear for UNI. -20 to 125C
YES
Trend is linear FOR BIP in previous paper by Jiahao “Correct Extrapolation…” for -20 to 85C
UNI+ and UNI- Ea matches after SH correction
Ea range = 0.18-0.28eV
0.92-0.98V
Ea range = 0.17-0.19eV
0.92-0.98V

## Slide 16: Open question 1: Arrhenius or not?
In Wu et al. 2012 “Temperature Dependence of TDDB Voltage Acceleration in High-κ/ SiO2Bilayers and SiO2 Gate Dielectrics” talks about non-Arrhenius trends in HfO2 stacks. The paper DOES NOT have a single plot of Ea - versus - voltage or field because extracting Ea makes no sense.
Wu et al. 2013 “Generalized hydrogen release-reaction model for the breakdown of modern gate dielectrics” clearly claims that to PROVE that field and current both play a role in the BD process, we should be observing non-Arrhenius trends.

## Slide 17: Open question 2: Two Ea regimes
*Assuming Arrhenius is true.
We observe two Ea regimes that are unexplained. (Could be due to mechanical causes)
To remove UNI cases. Can plot in MV/cm units instead.
Gradient = dipole moment*permittivity. Gradient has a physical meaning. Suspect dipole moment.
Left plot is with Jiahao’s SH correction which assumes ΔTSH is uniform for all ambient temperatures.
*Lines are visual aids
*Lines are visual aids
Blue and green lines seem parallel
*key plot

## Slide 18
Group Meeting
An ab initio study on the formation energy (Ef) of MgO
Reporter：Tong Su
Supervisor：Prof Ang Yee Sin
Date：06/12/2021

## Slide 19
Fang-Guang Kuang et al. 2017 An ab initio study on the electronic and magnetic properties of Mg0 with intrinsic defects
Calculation theory

## Slide 20
4.19793(0) Å
4.29596(0) Å
Toten Energy=-34.71809618 eV
Toten Energy=-34.71809618 eV eV
3-layer test

## Slide 21
6.36825(0) Å
6.36825(0) Å
Toten Energy=-46.63555909 eV
Toten Energy=-46.63555909 eV
4-layer test

## Slide 22
O
2X2X2 supercell bulk MgO (cubic)

## Slide 23
O-vacancy
O-rich:
Ef=6.712164 eV
Mg-rich:
Ef=1.208855 eV
O vacancy in 2X2X2 supercell MgO (cubic)

## Slide 24
O-rich:
Ef=8.117685 eV
Mg-rich:
Ef=8.117685 eV
B doping in 2X2X2 supercell MgO (cubic)

## Slide 25
O-rich:
Ef=12.09441 eV
Mg-rich:
Ef=5.152813 eV
B substitute O in 2X2X2 supercell MgO (cubic)
B substituent O

## Slide 26
O-vacancy
O-rich:
Ef=17.68484 eV
Mg-rich:
Ef=6.678223 eV
B substitute O nearby O vacancy in 2X2X2 supercell MgO (cubic)
B substitute O

## Slide 27
 |  | O-rich(Ef) | Mg-rich(Ef)
2X2X2MgO(bulk) | -381.3264188 |  | 
O-defect | -369.666255 | 6.71216383 | 1.20885536
B doping | -379.8881335 | 8.11768531 | 8.11768531
O-B doping | -370.9634125 | 12.09440633 | 5.15281255
2O-B doping | -360.4249784 | 17.68484044 | 6.6782235
bulk MgO | -11.9140852 |  | 
cubic bulk Mg | -1.46277673 |  | 
μ(O) | -4.948 |  | 
μ(B) | -6.6794 |  | 
Calculation original data

## Slide 28
3X3X1 supercell MgO (cubic)

## Slide 29
O vacancy in 3X3X1 supercell MgO (cubic)
O-rich(Ef) | Mg-rich(Ef)
6.57355848 | 1.07025001

## Slide 30
B doping in 3X3X1 supercell MgO (cubic)
O-rich(Ef) | Mg-rich(Ef)
5.54999535 | 5.54999535

## Slide 31
B substitute O in 3X3X1 supercell MgO (cubic)
O-rich(Ef) | Mg-rich(Ef)
11.66579919 | 6.16249072

## Slide 32
B substitute O nearby O vacancy in 3X3X1 supercell MgO (cubic)
O-rich(Ef) | Mg-rich(Ef)
17.10775361 | 6.10113667

## Slide 33
 |  | O-rich(Ef) | Mg-rich(Ef)
3X3X1MgO(4-layer) | -419.7621278 |  | 
O-defect | -408.2405693 | 6.57355848 | 1.07025001
B doping | -420.8915324 | 5.54999535 | 5.54999535
O-B doping | -409.8277286 | 11.66579919 | 6.16249072
2O-B doping | -399.4377741 | 17.10775361 | 6.10113667
bulk MgO | -11.9140852 |  | 
cubic bulk Mg | -1.46277673 |  | 
μ(O) | -4.948 |  | 
μ(B) | -6.6794 |  | 

## Slide 35
O-O vacancies distance |  |  | O-rich(Ef)(eV) | Mg-rich(Ef)(eV)
2.997Å | 2O vacancies（1） | -358.0973867 | 13.3330321 | 2.32641516
4.238Å | 2O vacancies（2） | -357.9818072 | 13.44861162 | 2.44199468
5.994Å | 2O vacancies（3） | -357.9980506 | 13.43236824 | 2.4257513
5.191Å | 2O vacancies（4） | -357.9869458 | 13.44347304 | 2.4368561
7.341Å | 2O vacancies（5） | -357.9976899 | 13.43272894 | 2.426112

## Slide 36
Thank YOU！

## Slide 37: Kinetic Monte Carlos Algorithm
M. Andersen et al. Front. Chem. 2019 A Practical Guide to Surface Kinetic Monte Carlo Simulations

## Slide 38
Kristen A. Fichtorn Kinetic Monte Carlo Simulations and Applications

## Slide 39: 31 Jan 2022 Agenda
Issue 0: Review of simulated sanity check
Issue 1: How best to define the increase in k due to neighboring defects?
Issue 2: How to account for the asymmetric pulsing of BIP?
Issue 3: How to model diffusion model?
Issue 0: Review of simulated sanity check
Issue 1: How best to define the increase in k due to neighboring defects?
Issue 2: How to account for the asymmetric pulsing of BIP?
Issue 3: How to model diffusion model?

## Slide 40
Issue 0
Review of simulated sanity check

## Slide 41
kB
Bulk cell Intrinsic rate
Kinetic Monte Carlos simulation
200 devices per plot
50 x 50 x 5 (X Y Z) size grid

## Slide 42
kI
kB
Interface cell Intrinsic rate
Bulk cell Intrinsic rate
kI = n*kB
Where n=1, 1.5, 2, 2.5, 3…
n=1.5
n=2
n=3
n=5.5
1100 devices per plot
50 x 50 x 5 (X Y Z) size grid

## Slide 43
kI
kB
Interface cell Intrinsic rate
Bulk cell Intrinsic rate
kI = n*kB
Where n=1, 1.5, 2, 2.5, 3…
n=1.5
n=2
n=3
n=5.5
1100 devices per plot
50 x 50 x 5 (X Y Z) size grid

## Slide 44
kI
kB
Interface cell Intrinsic rate
Bulk cell Intrinsic rate
kI = n*kB
Where n=1, 1.5, 2, 2.5, 3…
n=1.5
n=2
n=3
n=5.5
1100 devices per plot
50 x 50 x 5 (X Y Z) size grid
Surface roughness modeling

## Slide 45
Chart: n
| 1.5 | 2 | 2.5 | 3 | 3.5 | 4 | 4.5 | 5 | 5.5
 | 5.8555 | 5.3738 | 5.3922 | 5.2423 | 5.2504 | 5.2098 | 4.8235 | 5.0641 | 4.8529
Chart: n
| 1.5 | 2 | 2.5 | 3 | 3.5 | 4 | 4.5 | 5 | 5.5
 | 0.055715 | 0.05097 | 0.047864 | 0.045182 | 0.043773 | 0.041827 | 0.040719 | 0.039633 | 0.03897

## Slide 46
Chart: MTTF
| 1.5 | 2 | 2.5 | 3 | 3.5 | 4 | 4.5 | 5 | 5.5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19
 | 0.055715 | 0.05097 | 0.047864 | 0.045182 | 0.043773 | 0.041827 | 0.040719 | 0.039633 | 0.03897 | 0.038127 | 0.036733 | 0.035246 | 0.034919 | 0.033089 | 0.032324 | 0.0324 | 0.030917 | 0.031091 | 0.030612 | 0.030871 | 0.030014 | 0.030151 | 0.03005
Chart: Beta
| 1.5 | 2 | 2.5 | 3 | 3.5 | 4 | 4.5 | 5 | 5.5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19
 | 5.8555 | 5.3738 | 5.3922 | 5.2423 | 5.2504 | 5.2098 | 4.8235 | 5.0641 | 4.8529 | 4.7276 | 5.0598 | 4.6357 | 4.8962 | 4.3091 | 4.5022 | 4.3539 | 4.324 | 4.0806 | 4.2802 | 4.2003 | 3.9408 | 4.2396 | 4.1245

## Slide 47
Chart: Alpha = 1
| 10 | 3 | 4 | 5 | 6 | 7 | 8 | 9
 | 8.8752 | 2.9588 | 4.0293 | 4.2757 | 5.2683 | 6.2174 | 6.82 | 7.4374
Chart: Alpha = 5
| 10 | 3 | 4 | 5 | 6 | 7 | 8 | 9
 | 7.7404 | 2.7127 | 3.7669 | 4.1327 | 4.3079 | 5.3003 | 6.5885 | 6.1253

## Slide 48
Issue 1
How best to define the increase in k due to neighboring defects?

## Slide 49
kI
kB
Interface cell Intrinsic rate
Bulk cell Intrinsic rate
Proposed Solution

## Slide 50
kI+α1
kI+α1
kB+α1
kB+α1
kB+α1
Defect
αcount = function(count of neighboring defects)
Where function is tbc:
Polynomial
Log
Power
Exponential
Look up table (from Yee Sin’s DFT)
Proposed Solution

## Slide 51
kI+α2
kI+α2
kB+α2
kB+α2
kB+α1
kB+α1
kB+α1
Defect
αcount = function(count of neighboring defects)
Where function is tbc:
Polynomial [A*count^2+B*count+C]
Log [A*log(B*count+C)]
Power [A(count+C)^B]
Exponential [A*(exp(B*count+C))]
Look up table (from Yee Sin’s DFT)
Proposed Solution

## Slide 52
Issue 2
How to account for the asymmetric pulsing of bipolar pulsing (BIP)?

## Slide 53: Context
BIP pulsing is a repeated two step process.
Up (AP)  Down (P)  Up (AP)  Down (P)  …
Resistance for Up and Down are not the same. Ie. the k for defects are different.
BIP pulsing is a repeated two step process.
Up (AP)  Down (P)  Up (AP)  Down (P)  …
Resistance for Up and Down are not the same. Ie. the k for defects are different.

## Slide 54
Process step no. = 1, 3, 5…
Process step no. = 2, 4, 6…
Bulk rate 1
Bulk rate 2
Interface rate 1
Interface rate 2
Proposed Solution

## Slide 55
Bulk rate 1
Bulk rate 2
Interface rate 1
Interface rate 2
Proposed Solution
Process step no. = 1, 3, 5…
Process step no. = 2, 4, 6…

## Slide 56: Problems
Physically inaccurate. BIP timestep is different from defect generation timestep. Ie. in one Up pulse, more than one defect can be generated.
Physically inaccurate. BIP timestep is different from defect generation timestep. Ie. in one Up pulse, more than one defect can be generated.

## Slide 57
kI_bottom
kB
Interface cell Intrinsic rate
Bulk cell Intrinsic rate
kI = n*kB
Where n=1, 1.5, 2, 2.5, 3…
kI_Top

## Slide 58
Issue 3
How to model diffusion model?

## Slide 59
kI
kI
kI
kI
kI
kB
kB
kB
kB
kB
kB
kB
kB
kB
kB
kB
kB
kB
kB
kB
0
0
0
0
0
Proposed Solution
kB
kI
kI
kI
kB
kB
kB
kB
kB
kB
kB
kB
kB
kB
kB
kB
kB
kB
kB
0
0
0
0
0
kd
Defect generation
kd
kd

## Slide 60
kB
kI
kI
kI
kB
kB
kB
kB
kB
kB
kB
kB
kB
kB
kB
kB
kB
kB
kB
0
0
0
0
0
Proposed Solution
kd
kI
kI
kI
kI
kI
kB
kB+α
kB+α
kB
kB
kB+α
kB+α
kB+α
kB
kB
kB
kB
kB
kB
kd
kd
kd
0
0
0
0
0
Defect activation
kd
kd

## Slide 61
kB
kI
kI
kI
kI
kB
kB
kB
kB
kB
kB
kB
kB
kB
kB
0
0
0
0
0
Proposed Solution
kI
kI
kI
kI
kI
kB
kB+α
kB+α
kB
kB
kB+α
kB+α
kB+α
kB
kB
kB+α
kB+α
kB+α
kB
kd
kd
kd
0
0
0
0
0
Defect diffusion for unipolar
kB
kB+α
kB+α
kB
kd
kd
kd
kd
kd
kd
kd

## Slide 62
kB
kI
kI
kI
kI
kB
kB
kB
kB
kB
kB
kB
kB
kB
kB
0
0
0
0
0
Proposed Solution
kI
kI
kI
kI
kI
kB
kB+α
kB+α
kB
kB
kB+α
kB+α
kB+α
kB
kB
kB+α
kB+α
kB+α
kB
kd
kd
kd
0
0
0
0
0
Defect diffusion for bipolar
kB
kB+α
kB+α
kB
kd
kd
kd
kd
kd
kd
kd
kd
kd
kd
kd
kd

## Slide 63
kI
kI
kI
kI
kI
kB
kB+α
kB+α
kB
kB
kB+α
kB+α
kB+α
kB
kB
kB
kB
kB
kB
Proposed Solution 1
kd
kd
kd
0
0
0
0
0
kI
kI
kI
kI
kI
kB+α
kB+α
kB+α
kB
kB+α
kB+α
kB+α
kB
kB+α
kB+α
kB+α
kB
kB
kd
kd
kd
0
0
0
0
0
Defect damage
kd
kd
kd
kd
kd
kd
kd
kd

## Slide 64
kI
kI
kI
kI
kI
kB
kB+α
kB+α
kB
kB
kB+α
kB+α
kB+α
kB
kB
kB
kB
kB
kB
Proposed Solution 2
kd
kd
kd
0
0
0
0
0
kI
kI
kI
kI
kI
kB+α
kB+α
kB+α
kB
kB+α
kB+α
kB+α
kB
kB+α
kB+α
kB+α
kB
kB
kd
kd
kd
0
0
0
0
0
Defect damage that results in a non-mobile defect (purple)
kd
kd
kd

## Slide 65
kI
kI
kI
kI
kI
kB
kB
kB
kB
kB
kB
kB+α
kB+α
kB+α
kB
kB
kB+α
kB+α
kB
Proposed Solution
0
0
0
0
0
kd
kI
kI
kI
kI
kI
kB
kB
kB
kB
kB
kB
kB
kB
kB
kB
kB
kB
kB
kB
kB
0
0
0
0
0
Defect termination
kd
kd
kd
kd

## Slide 66
Proposed Solution
kI
kI
kI
kI
kI
kB
kB+α
kB+α
kB+α
kB
kB
kB+α
kB+α
kB
kB
kB+α
kB+α
kB+α
kB
0
0
0
0
0
0
0
0
0
0
kI
kI
kI
kI
kI
kd
kd
kd
kB
kB+α
kB+α
kB+α
kB
kB
kB+α
kB+α
kB
kB
kB+α
kB+α
kB+α
kB
kd
kd
kd
kI
kB+α
kB
kd
kI
kB+α
kd
kB
Bulk rate 1
Bulk rate 2
Interface
rate 1
Interface
rate 2
α 1
α 2
Diffusion
rate 1
Diffusion
rate 2
Asymmetry
kd
kd
kd
kd

## Slide 67: DFT simulation for LUT
1
2
3
4
Ef
5
6
7
8
Format:
Ef = Dictionary{Positions: Efpositions}
Example:
Ef = Dictionary{0: Ef0;
1: Ef1; 2: Ef2; 3: Ef3; …
1,2: Ef1,2; 1,3: Ef1,3; 1,4: Ef1,4; …
1,2,3: Ef1,2,3; 1,2,4: Ef1,2,4; …
…
1,2,3,4,5,6,7,8: Ef1,2,3,4,5,6,7,8}
2D illustration

## Slide 68: Possible Model BIP
Diffusion/Drift
*Would there a shielding effect?
Induced
Neighbor
Diffusion/Drift
Induced
Neighbor
Gap to Top Electrode
Gap to Btm Electrode
How does E-field or Current worsen Induced Neighbor or Diffusion/Drift?
BIP is Arrhenius. Ie. Higher temp accelerates single process. Dominant single process.
Induced Neighbor and Diffusion are working together model below
Missing: explanation for the kink in H vs V
Combined gap is smaller than UNI
Shorter TTF
Initial state has some defects
Are most of the initial defects at the interface?
Do most of the defects form at the interface?

## Slide 69: Possible Model UNI
Diffusion/Drift
*Would there a shielding effect?
Induced
Neighbor
Induced
Neighbor
Diffusion/Drift
Gap to Top Electrode
Gap is larger than BIP
 Longer TTF
How does E-field or Current worsen Induced Neighbor or Diffusion/Drift?
UNI is non-Arrhenius. Ie. Higher temp accelerates multiple processes. No dominant single process.
Induced Neighbor and Diffusion are working against each other in model below
UNI MTTF approaches BIP MTTF at higher temp.
Main difference in UNI+ and UNI- is SH.
Might be harder for defects to diffuse at the interface due to lattice mismatch
Initial state has some defects
Are most of the initial defects at the interface?
Do most of the defects form at the interface?

## Slide 70: We model the O defects as BCC about a reference Oxygen atom
https://msestudent.com/what-is-the-difference-between-fcc-and-bcc-crystal-structure-properties-interstitial-sites-and-examples/

## Slide 72
350 * 350 * 5 thickness
Virtual O, will not form defect

## Slide 73
350 * 350 * 5 thickness

## Slide 74
350 * 350 * 5 thickness